Door gear 3D Printing Settings

Filament

PLA
Diameter - 1.75 (mm)
Flow - 100%

----------------------------------------------------------------------------------------------------------------------------

Quality

Layer Height - 0.2 (mm)
Initial Layer Thickness - 0.3 (mm)
Shell Thickness - 0.8 (mm)
Bottom/Top Thickness - 1.2 (mm)
Fill Density - 20 (%)

----------------------------------------------------------------------------------------------------------------------------

Speed and Temperature

Print Speed - 50 (mm/s)
Travel Speed - 90 (mm/s)
Bottom Layer Speed - 30 (mm/s)
Printing Temperature - 215 (C)
Bed Temperature - 60 (C)

----------------------------------------------------------------------------------------------------------------------------

Support Type

None / Touching Buildplate / Everywhere
Platform Adhesion Type - None / Brim / Raft